## Slide 1
Focused-ion-beam-milled GaAs nanotip: A semiconducting ultrafast photoemission electron source
Sam Keramati1,*, William Newman1, Herman Batelaan1, T. J. Gay1
S. Keramati, W. Newman, and T. J. Gay acknowledge support by NSF under the Award Number PHY-2110358. H. Batelaan acknowledges support by NSF under the award number PHY-1912504.
*Present address (S.K.): Departments of Physics and Chemistry, University of Toronto, Canada. Email: sam.keramati@utoronto.ca
10 μm
Fig.1 SEM image of a cleaved GaAs shard
Cleaved GaAs tips contain several sharp (nano)structures which may photoemit under fs laser illumination. We seek to achieve well-defined GaAs nanostructures as ultrafast spin-polarized free electron sources [1-2].
Fig.2 Focused ion beam (FIB) milled GaAs tip
A nanotip is carved out in a 3D Ga+ ion milling process (FEI Helios 660). The geometrical apex radius of curvature is 70 nm.
Femtosecond photoemission properties of this tip are presented.
We also demonstrate workfunction lowering using a cesium dispenser in the proximity of this tip.
References
[1] E. Brunkow, et al., "Femtosecond-laser-induced spin-polarized electron emission from a GaAs tip", Appl. Phys. Lett. 114, 073502 (2019).
[2] T.J.Gay, et al., U.S. Patent 1011337, "Fast Spin-Polarized Electron Source.”
1Department of Physics and Astronomy, University of Nebraska-Lincoln, USA
Fig.3 Multiphoton photoemission order varies with the cesiator current
Photoemission order n decreases as the deposition rate of Cs on the GaAs tip increases (red data). Ti:Sa oscillator at 90 MHz, <100 fs, 800nm (1.55 eV), <10 GW/cm2. Vtip = -100 V. Workfunction = 4.1 eV.
Activation by Cs decreases the workfunction of GaAs. The total multiphoton energies are shown in parentheses. Large lowered values of up to -1.78 eV for moderate currents are thus demonstrated. Increase in emission current is consistently observed from <2 e/pulse for unactivated tip to up to 8 e/pulse. The tip remains activated (black data).
Activated
Deactivated
Fig.4 Count rate stability
The photoemission count rate as well as the emission current off the tip show a transient behavior for the activated tip for the first several seconds after unblocking the laser. We attribute this to fs laser ablation of the deposited Cs layer.
Deactivating the tip by leaving it in the same fs laser focal spot for 6 hours at ICs = 0 A leaves no Cs for ablation, hence steady photoemission.
laser blocked
laser blocked
laser unblocked
laser unblocked